## Slide 1: BATTERIES AND TYPES

## Slide 2
 General aspects on power systems
 Classification of batteries
 Classical examples of power systems
 Special view on lead-acid system
 About lithium batteries

## Slide 3: BATTERY - cell - power packs - power sources
Is a source of energy, obtained by the conversion of chemical energy from chemical reaction into electrical energy
Thus BATTERIES represent a silent form of energy producing chemical devices, which generate electricity on demand

## Slide 4: Hype on Batteries…?
The rapidity with which energy resources and oil fields are consumed at present and in the future will depend on the rapidity with which regions of the world industrialize, the rate of population growth, the ultimate level of human desires to possess material goods and the effort that is made to accelerate production
The growing concern with managing the costs of military, space crafts, portable electronics, implantable medical devices,
communication technology etc.,
The importance of preserving our green environment mainly because of the very high rate of industrialization, modernization and partly due to population explosion etc., has placed an increased emphasis on efficient power sources
SO…. BATTERIES…. Boon….. For energy re-regeneration

## Slide 5
CATHODE
ANODE
ELECTROLYTE
SEPARATOR
CONTAINER

## Slide 6: CELL CONSTRUCTION
ELECTROLYTE
SEPARATOR
CONTAINER
ANODE
CATHODE

## Slide 7: CELL REACTIONS IN A BATTERY SYSTEM
ANODE REACTION: is an oxidation reaction which releases electrons (Anode is the –ve electrode in EC cell)
CATHODE REACTION: is a reduction reaction which consumes electrons (Cathode is the +ve electrode in EC cell)
ELECTROLYTE is an ion-conducting medium which conducts ions between the electrodes so that the above reactions can take place

## Slide 8: WORKING PRINCIPLE
V
A
e-
_
+

## Slide 9: CLASSIFICATION OF BATTERIES
1.PRIMARY BATTERY
- for single use only
2. SECONDARY BATTERY
- for repeated use

## Slide 10: 1. PRIMARY BATTERY
- Non-rechargeable (cell reactions are irreversible)
- Self-discharges whether used or not
LECLANCHE CELLS (Zn/C) - Popular low-cost system
Applications: Torch light, portable radios, toys, novelties, etc.
Mg/MnO2 CELLS - High capacity system
Applications: Military communication equipment, voting machines, etc.

## Slide 11: RESERVE BATTERY
- one of the cell components, usually the electrolyte, is kept isolated from the rest and is added at the time of need
Mg/Cu2Cl2, Mg/AgCl (sea water activated battery) Applications: Torpedoes, Sea beacons (Mainly in Meteorology and Defence fields)
Li/FeS2 (Thermally activated battery) Applications: In Missiles

## Slide 12: 2. SECONDARY BATTERY
- Rechargeable (cell reactions are reversible)
Lead-Acid Battery (Pb/H+) Nickel-Cadmium Battery (Ni-Cd) Nickel-Iron Battery (Ni-Fe)
Nickel-Metal hydride Battery (Ni-MH) Lithium battery (Li-LiMxOy)
Lithium-Ion battery (C-LiMxOy)
Lithium-Ion Polymer Battery (C-LiMxOy)

## Slide 13: LEAD-ACID BATTERY
: Pb
: PbO2
: H2SO4
: 2.0 V
ANODE CATHODE
ELECTROLYTE CELL VOLTAGE
APPLICATIONS:
AUTOMOTIVE STARTING--LIGHTING--IGNITION (SLI), ELECTRIC VEHICLES, EMERGENCY POWER UTILITIES, PORTABLE TOOLS, INDUSTRIAL TRUCKS, ETC.

## Slide 14: LITHIUM SECONDARY BATTERY
ANODE CATHODE
ELECTROLYTE CELL VOLTAGE
: Li METAL
: LiCoO2
: LiPF6 in EC:PC
: 4 V
APPLICATIONS:
ELECTRIC VEHICLES, PORTABLE ELECTRONIC DEVICES, ETC.

## Slide 15: LITHIUM-ION BATTERY
ANODE CATHODE
ELECTROLYTE CELL VOLTAGE
: CARBON
: LiCoO2
: LiPF6 in EC:PC
: 4 V
APPLICATIONS:
ELECTRIC VEHICLES, CELL PHONES, CAMCORDERS, LAP-TOP AND PALM- TOP COMPUTERS, PORTABLE ELECTRONIC DEVICES, ETC.

## Slide 16: LITHIUM-POLYMER BATTERY
ANODE CATHODE
: Li
: LiCoO2
ELECTROLYTE : SOLID POLYMER FILMS CELL VOLTAGE : 4 V
APPLICATIONS:
ELECTRIC VEHICLES, CREDIT CARDS, SLIM ELECTRONIC DEVICES, ETC.

## Slide 17: LITHIUM-ION POLYMER BATTERY
ANODE CATHODE
: CARBON
: LiCoO2
ELECTROLYTE : SOLID POLYMER FILMS CELL VOLTAGE : 4 V
APPLICATIONS:
ELECTRIC VEHICLES, PORTABLE ELECTRONIC DEVICES, ETC.

## Slide 18: LEAD-ACID BATTERY
ANODE CATHODE
ELECTROLYTE CELL VOLTAGE
: Pb
: PbO2
: H2SO4
: 2.0 V

## Slide 19: At positive plate:
2PbSO4 + 2H2O Pb + 2H2SO4 + PbO2
REACTIONS DURING CHARGING
Discharge
PbSO4 + 2H2O PbO2 + 4H+ + SO42- + 2e-
2H2O O2 + 4H+ + 4e-
At negative plate:
PbSO4 + 2e-  Pb + SO42- 2H+ + 2e-  H2
OVERALL CELL REACTION
Charge

## Slide 20: The success of Pb/H+ battery is due to:
Raw material is cheap and also can be recovered from scrap (spent batteries)
Supply of high power over a wide range of temp. Very high reversibility
Availability of mass production techniques Availability of multifarious battery configurations Maintenance free

## Slide 21: BATTERY TESTING METHODS FOR Pb/H+ BATTERIES
 Air Pressure test (A check for cell sealing)
 Capacity test
 High rate discharge test
 Charge retention test
 Over charge resistance test (determining the life or
health of the grid materials)
 Life test (determining life or health of the +ve or
-ve plate active material)
 Vibration test

## Slide 22: CHARGING PROCEDURES
Constant current or galvanostatic charging (single step, two step, multistep galvanostatic charging)
Constant voltage charging Controlled current-voltage charging Modified constant-voltage charging Tapered charging
Boost charging Trickle charging Float charging Equalizing charging Pulse charging
Gas controlled charging

## Slide 23
FACTORS AFFECTING BATTERY PERFORMANCE AND LIFE
***
The cathode/anode composition, its design, nature and characteristics of the oxide, composition of paste, curing, formation and initial charging methods, concentration of the acid, the separators, rate of discharge and temperature of operation
Particle size, surface area, water and acid absorption rate, plate porosity, crystallography of the oxide etc.,

## Slide 24: Failure of Pb/H+ batteries due to:
 Long standing in discharged condition
 Too high acid concentration
 Prolonged under-charging
 Increased self-discharge
 Continuous operation between 40 & 50C

## Slide 25: PROBABLE TYPES OF DEFECTS IN Pb/H+ BATTERIES
Positive plate corrosion Shedding of active materials Short circuting
Sulfation Lagging of cells
Failure of separator
Growth and buckling of plates Explosion

## Slide 26: MAINTENACE AND HEALTH MONITORING PROCEDURES FOR Pb/H+ BATTERIES
Wiping off the dirt (can lead to self discharge)
Checking the containers and sealing components for crack or seepage
Checking the cables for ensuring good contact with the terminals
Checking and cleaning of the vent holes in the plugs Checking the electrolyte level
Checking the temperature of theelectrolyte Measurement of specific gravity of the electrolyte, cell
voltages, plate potentials by using cadmium electrode and
temperature of the electrolyte particularly at the end of charging and discharging

## Slide 27: LITHIUM BATTERY – SALIENT FEATURES
o High working voltage (>3.8V)
o High inherent capacity (>150mAh/g)
o High energy density (>100Wh/Kg)
o Wide electrochemical window (2.5V - ~5V)
o Wide operating temperature (-40 - +80o)
o Light weight (variable with configuration)
o Long shelf-life (~8 years)

## Slide 28: CATHODE MATERIALS FOR RECHARGEABLE LITHIUM/LITHIUM-ION BATTERIES
***
3-volt (e.g. LiMnO2)
4-volt (e.g. LiCoO2, LiNiO2, LiMn2O4) 5-volt (e.g. LiNiVO4)
1 Li-ion battery = 3 Ni-Cd / Ni-MH

## Slide 29: INTERCALATION

## Slide 30: SOLID POLYMER ELECTROLYTES FOR Li-ION CELLS
*** HOMOPOLYMERS e.g., PVdF
BLEND POLYMERS e.g., PVC-PVdF COPOLYMERS e.g., PVdF-HFP (KYNAR)

## Slide 31: GLOVE BOX
MOISTURE and OXYGEN LEVEL < 20ppm

## Slide 33: NEED FOR BATTERY OPERATED VEHICLES (Electric Vehicles - EV)

For conserving natural fuel sources

Decreased air & noise pollution
Battery driven vehicles provide efficient transportation in the near future

## Slide 34: CRITERIA OF BATTERY SYSTEMS FOR EV APPLICATIONS
High energy density High power density Good cycle life
Wide temp. range of operation (-30 to +70oC) Quick recharge
Totally unassisted and maintenance free nature Tolerance to abuse
Non-toxicity of battery materials Safety & reliability, non-polluting

## Slide 35: EV PARAMETERS DECIDING THE BATTERY SPECIFICATIONS AND POWER REQUIREMENTS
 Vehicle range
 Vehicle acceleration
 Gross vehicle weight
 Tyre rolling resistance
 Electric motor efficiency
 Hill climbing capacity

## Slide 36: RECENT TRIALS WITH Ni-MH BATTERY UNDER APPROPRIATE DRIVING CONDITIONS
Sp. Energy = 70-80Wh/Kg
Range = 200miles peak speed = 90miles/h

## Slide 37: ELECTRIC VEHICLE
NISSAN ALTRA ELECTRIC CAR
POWERED BY SONY LITHIUM- ION BATTERY 120 MILES/CHARGE; SPEED: 60miles/ h

## Slide 38
MATSUSHITA HITACHI-MAXEL EVEREADY
MAKERS OF POWER SYSTEMS – ALL TYPES SANYO
TOSHIBA
JAPAN
SONY, PANASONIC, GEC, OVONIC — USA
EAGLE-PICHER, VARTA - GERMANY SAFT – FRANCE, CHINA, KOREA, USA

## Slide 39: THANK YOU ALL